Appendix 3: The Late Iron Age Pottery

R.S.Leary

# Factual Data

The pottery was examined and catalogued according to the Guidelines of the Study Group for Romano-British Pottery for basic archiving (Darling 2004).  The fabrics were recorded in broad groups and details of the fabrics are described below.  Reference was made to the Lincolnshire fabric collection codes.  Details of fabric variations were recorded where appropriate.  Forms were described.

## Quantity and provenance

35 sherds of pottery were recovered from the site.  The condition of the pottery was good.  Most of the sherds were of average weight but most of a bead rim jar came from context 803 with one large sherd giving an almost complete profile.  Most of the pottery came from feature 804.

| Context | Feature | Sherd count | Sherd weight | Rim % values |
| --- | --- | --- | --- | --- |
| 11-102 | Linear assoc with 1300 | 1 | 2.7 |  |
| 1202 | Enclosure, probably same as 1300 | 5 | 43.9 |  |
| 13-101 | Fill of 1300 | 1 | 12 |  |
| 16-101 | Fill of 1300 | 3 | 29.3 |  |
| 16-103 | Fill of scoop within 1300 | 4 | 26.1 | 5 |
| 802 | Fill of 801 | 1 | 3.7 |  |
| 803 | Top fill of 804, internal feature in 801 | 16 | 420.3 | 34 |
| 817 | Primary fill of 804, internal feature in 801 | 3 | 42.2 | 4 |
| Unstrat. |  | 1 | 2.6 |  |
|  |  | 35 | 582.8 | 43 |

Table 1 Quantification of pottery by context

## Range and variety of material

### Wares

Only six ware groups were identified, three shelly wares with one variant, two quartz-tempered wares and a white ware.  The most common fabric was a reduced shell-tempered ware with moderate quantities of medium sized shell.  This fabric was occasionally oxidised but this could easily be a variant of the same basic fabric due to firing conditions rather than a distinct fabric.  Indeed some sherd were reduced outside and oxidised inside.  A group of sherds from 1202 had rather coarser sherds than the other CTB1 sherds.  Within this group was a sherd which may be part of a storage jar rim.  Storage jars often were given coarser temper so this group is separated out as a second shell-tempered fabric.  Two sherds from 802 and 803 had sparse fine shell and moderate quartz inclusions.  This is a fabric commonly use to make bowls, often carinated and with cordons, of late Iron Age type.  The quartz tempered wares were less common.  These were divided into coarse and medium.  Only one example of each was found: a jar with bevelled rim from 16-103 has medium quartz inclusions, a rounded rim jar from 803 had abundant medium to coarse quartz inclusions and an unstratified scrap had medium quartz inclusions.  Lastly the white sherd from 803 compared well with samples of North Gaulish white ware in the fabric series of York Archaeological Trust.  This fabric was used for butt beakers imported in the immediate pre-Conquest and post-Conquest period up to around AD70. Pre Conquest examples were present at Dragonby (Rigby 1996).

Figure 1 Relative quantities of fabric groups by sherd count, weight and estimated equivalents

### Forms

Apart from the imported vessel, perhaps a beaker or flagon, the identified vessels were predominantly ovoid jars with rounded rims, bevelled internally.  This internal bevelling is particularly characteristic of the late PRIA and Conquest period.  One PQTM vessel may be from a bowl with a concave side.  This and the white ware sherd are the only pieces belonging to table ware.  Burnt encrustations on the large fragment from 803 gives weight to the traditional interpretation of these vessels as cooking pots.  The CTB7 sherds may belong to a storage jar.

## Chronology

Most of the pottery was of a type common in the pre-Roman Iron Age (PRIA) which continued to be made in the early Roman period where it was used alongside Roman wheel-thrown pottery until the middle of the second century.  The absence of any sherds which demand a Roman date suggests that this settlement belongs to the PRIA.  The presence of a fine shell and quartz tempered ware typical of late Iron Age cordoned and carinated bowls in contexts 802 and 803 suggest the enclosure belonged to the late Iron Age-Conquest period.  A North Gaulish white ware sherd gives a similar date for context 16-103.  This sherd could date to the late Iron Age just before the Conquest or as late as c70AD.  Its lack of diagnostic features precludes close dating.  The CTB1 jar forms belong to the simple native type which is exceptionally long lived in Lincolnshire (Elsdon 1996, type 20).  The internal bevelling of the rim, grooves on the neck and rim and hints of wheel finishing suggests a date in the late Iron Age for most of these vessels.  The quartz-tempered vessels may be slightly earlier in date.  The heavily tempered rim sherd from 803 lacks the careful finishing of the CTB1 jars and may be of middle Iron Age date.  The fine quartz tempered jar from 103 was associated with the North Gaulish import sherd.  This jar has a burnished rim and internal bevel like the CTB1 jars and may of similar date range.  A date in the late Iron Age just before the Roman arrived in the region would be consistent with these types.

## Function and site status

The pottery is typical of rural settlement of the late Iron Age.  The presence of an imported sherd raises the possibility of a higher status settlement as such imports are uncommon on rural sites.  The rest of the assemblage and the near complete absence of any tableware may indicate that any settlement of higher social status may have been sited some distance from the excavations.

# Statement of potential and recommendation

The significance of this pottery assemblage is enhanced considerably by the presence of the imported sherd and the good condition of the pottery.

# Storage and curation

The pottery is stable but shell tempered pottery is prone to flaking so the sherds should be wrapped with care within their storage box.

# Bibliography

Darling, M.J. 2004 Guidelines for the archiving of Roman pottery.  Journal of Roman Pottery Studies Vol 11, 67-75.

Elsdon, S., 1996 Iron Age pottery, in J. May, Dragonby, Report on Excavations at an Iron Age and Romano-British Settlement in North Lincolnshire, Oxbow Monograph 61, 1996, 400-511.

Rigby, V. 1996 Imported Pottery and Close Imports.  In J. May, Dragonby, Report on Excavations at an Iron Age and Romano-British Settlement in North Lincolnshire, Oxbow Monograph 61, 1996, 587-97.

Tomber, R. and Dore, J., 1998, The National Roman Fabric Reference Collection.  A Handbook, MoLAS Monograph 2.  London

Appendix 1 Pottery quantification values

| Fabric | Sherd count | Sherd weight | Rim % value | Fabric description | Lincs fabric series code |
| --- | --- | --- | --- | --- | --- |
| CT | 2 | 2.4 |  | Shell-tempered | SHEL |
| CTB1 | 17 | 451.2 | 36 | Moderate, medium, shell. Brown | IASH |
| CTB1OX | 4 | 41.3 |  | Moderate, medium, shell. Oxidised surfaces | IASH |
| CTB7 | 3 | 38.5 |  | Abundant, ill-sorted fine to coarse shell. Orange-brown | IASHC |
| CTB8 | 2 | 8.3 |  | Sparse, fine shell and sparse, medium, subrounded quartz. Grey | IASHF |
| NOG WH1 | 1 | 2.4 |  | Very fine white ware with very fine quartz and rare red-brown inclusions. | GBWW |
| PQTC | 1 | 9.7 | 2 | Brown with grey core. Abundant, well-sorted, subangular quartz | IASA |
| PQTM | 5 | 29 | 5 | Grey. Rare fine shell and moderate, well-sorted, subangular fine to medium quartz. | ?IAMSH |

Table 1 Ware quantification

|  |  | Bowl | Jar |
| --- | --- | --- | --- |
| Fabric | Unk | Concave body | Closed vessel | Internally bevelled rim | Bead rim | Rounded rim, internally bevelled | Rounded rim |
| CT | 2 |  |  |  |  |  |  |
| CTB1 | 2 |  | 9 |  | 1 | 5 |  |
| CTB1OX | 1 |  | 3 |  |  |  |  |
| CTB7 |  |  | 3 |  |  |  |  |
| CTB8 | 1 | 1 |  |  |  |  |  |
| NOG WH1 | 1 |  |  |  |  |  |  |
| PQTC |  |  |  |  |  |  | 1 |
| PQTM | 1 |  | 1 | 3 |  |  |  |

Table 2 Form and ware quantification using sherd count

|  | Bowl | Jar |
| --- | --- | --- |
| Fabric | Concave body | Closed vessel | Internally bevelled rim | Bead rim | Rounded rim, internally bevelled | Rounded rim | Concave body |
| CT | 2.4 |  |  |  |  |  |  |
| CTB1 | 5.4 |  | 230.5 |  | 165 | 50.3 |  |
| CTB1OX | 12 |  | 29.3 |  |  |  |  |
| CTB7 |  |  | 38.5 |  |  |  |  |
| CTB8 | 4.6 | 3.7 |  |  |  |  |  |
| NOG WH1 | 2.4 |  |  |  |  |  |  |
| PQTC |  |  |  |  |  |  | 9.7 |
| PQTM | 2.7 |  | 2.6 | 23.7 |  |  |  |

Table 3 Form and ware quantification using sherd weight

| Autonumber | Trench | Context | Suitable for drawing | Fabric | Count | Weight | Abrasion | Part | Form | Vessel type | RimD | RimP | Condition | Vessel spot date | Comments | Dectec | Decmotif | Decpos | Dectec2 | Decmotif2 | Decpos2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 13 | US |  | PQTM | 1 | 2.6 | V | BDY | closed vessel | jar? |  |  |  | LIA |  | Grooved | single | outside body | burnished |  | outside body |
| 2 |  | 13-101 |  | CTB1OX | 1 | 12 | V | BDX |  | jar? |  |  |  | IA |  |  |  |  |  |  |  |
| 3 |  | 16-101 |  | CTB1OX | 3 | 29.3 | M | BDY | closed vessel | jar |  |  |  | IA |  |  |  |  |  |  |  |
| 4 |  | 1202 |  | CTB1 | 2 | 5.4 | V | BDX |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 |  | 802 |  | CTB8 | 1 | 3.7 | V | BDY | concave body | bowl? |  |  |  | LIA? |  | Burnished or smoothed |  | outside body |  |  |  |
| 6 |  | 1202 |  | CTB7 | 3 | 38.5 | A | BDY | closed vessel | jar |  |  |  |  |  |  |  |  |  |  |  |
| 7 |  | 803 |  | CTB1 | 3 | 21.7 | M | R+B | expanded rim with internal bevel | jar | 20 | 8 |  | LIA | Oxidised inside rim |  |  |  |  |  |  |
| 8 |  | 803 |  | CT | 2 | 2.4 | V | CR |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9 |  | 803 | Y | PQTC | 1 | 9.7 | A | R+B | rounded rim | jar |  | 2 |  | IA |  |  |  |  |  |  |  |
| 10 |  | 817 |  | CTB1 | 2 | 28.7 | M | BDY | closed vessel | jar |  |  |  | IA |  |  |  |  |  |  |  |
| 11 |  | 817 |  | CTB1 | 1 | 13.5 | M | RIM | expanded rim with internal bevel | jar | 22 | 4 |  | LIA | ? Same as jar from 803 |  |  |  |  |  |  |
| 12 |  | 11-102 |  | PQTM? | 1 | 2.7 | V | SCR |  |  |  |  |  | IA or RB | Could be grey ware |  |  |  |  |  |  |
| 13 |  | 16-103 | Y | PQTF | 3 | 23.7 | M | R+B | upright, internally bevelled rim | jar | 16 | 5 |  | LIA |  | Smoothed |  | outside body | burnished |  | over rim |
| 14 |  | 16-103 |  | NOG WH1 | 1 | 2.4 | A | BDX |  |  |  |  |  | LIA-CONQUEST |  |  |  |  |  |  |  |
| 15 |  | 803 | Y | CTB1 | 1 | 165 | U | R+B | bead rim with two grooves on external face of rim | jar | 15 | 19 | Burnt matter outside upper body | LIA-CONQUEST | Handmade |  |  |  |  |  |  |
| 16 |  | 803 |  | CTB1 | 7 | 201.8 | U | BDY | closed vessel | jar |  |  |  | LIA-CONQUEST | Probably part of above vessel |  |  |  |  |  |  |
| 17 |  | 803 | Y | CTB1 | 1 | 15.1 | M | RIM | expanded rim with internal bevel | jar | 16 | 5 |  | LIA-CONQUEST | same as jar from 817 |  |  |  |  |  |  |
| 18 |  | 803 |  | CTB8 | 1 | 4.6 | A | BDX |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Totals |  |  |  |  | 35 | 582.8 |  |  |  |  |  | 43 |  |  |  |  |  |  |  |  |  |